PRODUCT DATA SHEET

BFT-1001® PVC L BA

PVC Self Adhesive Membrane for Roofing Waterproofing

PRODUCT DESCRIPTION

BFT-1001®, is a multi-layer, self-adhesive, weldable sheet membrane with a factory applied butyl rubber adhesive backing and siliconize polyethylene release liner. Contains ultraviolet light stabilizers to provide a colour stable, fast installation, low maintenance and durable membrane.

Uses

Roof waterproofing membrane for exposed flat roofs on smooth substrates

CHARACTERISTICS/ADVANTAGE

- Factory applied VOC free self adhesive system

- Resistant to permanent UV radiation ▪

- High water vapour permeability ▪

- Hot air welded no naked flames ▪

- Fast installation ▪

- Instant wind uplift resistance through the self-adhesive back in

| PRODUCT INFORMATION |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Packaging |  | Standard rolls are wrapped individually |  |  |  |
| Roll size |  | Length 15,00 m Width 2,00 m |  |  |  |
| Structure |  | Top surface: PVC |  |  |  |
|  |  | Reinforce: none |  |  |  |
|  |  | Backing: Non-woven with butyl rubber adhesive |  |  |  |
| Shelf Life |  | 12 months from production date. |  |  |  |
| Storage Conditions |  | Product must be stored in original unopened and undamaged sealed packaging in dry conditions and temperatures between + 5 °C and + 35 °C. Protect from direct sunlight, rain, snow and ice, etc. Store in a horizontal position. Do not stack pallets of the rolls on top of each other, or under pallets of any other materials during transport or storage. Always refer to packaging |  |  |  |
| TECHNICAL INFORMATION |  |  |  |  |  |
| Tensile Strength |  |  | ≥120N/cm | GB-12952-2011 |  |
| Elongation |  |  | ≥150% |  |  |
| Foldability at Low Temperature |  |  | -25 |  |  |
| Peel strength of coil from aluminum sheet under standard conditions |  |  | ≥1.5N/MM | GB/T 23260-2009 |  |
| Heat resistance of self-adhesive surface |  |  | 70℃ |  |  |
| Tackiness |  |  | ≥15min |  |  |
| APPLICATION INFORMATION |  |  |  |  |  |
| Ambient Air Temperature | +5 °C min. / +60 °C max |  |  |  |
| Substrate Temperature | +5 °C min. / +60 °C max |  |  |  |
| Substrate Temperature | Waterproofing membrane not compatible with direct contact to other plastics, e.g. EPS, XPS & PF. Not resistant to tar, bitumen, oil and solvent containing materials. |  |  |  |

Results may differ based upon statistical variations depending upon mixing methods and equipment, temperature, application methods, test methods, actual site conditions and curing conditions.

APPLICATION INSTRUCTIONS

SUBSTRATE QUALITY

The substrate surface/supporting layer must be uniform, smooth and free of any sharp protrusion or burrs, clean, dry and free of grease, bitumen, oil and dust. All layers of the roof build-up and substrate must be secured against wind uplift

The substrate must be one of the following materials:

- OSB

- Plywood

APPLICATION METHOD / TOOLS

Welding overlap seams

All membrane seam overlaps must be welded by using hand welding guns and pressure rollers or automatic heat welding machines, with individually adjustable and electronically controlled welding temperatures.

LIMITATIONS

- Do not apply to wet, damp or unclean surfaces.

- Do not apply to slopes over 20°

- Installation of some ancillary products, e.g. contact adhesives / cleaners are limited to temperatures above +5 °C.

- Be aware special measures may be compulsory for certain installations below +5 °C ambient temperature due to safety and national regulations