PRODUCT DATA SHEET

BFT-1003® Roof Membrane

Excellent Outdoor Durability, Mechanical Impact Resistance

PRODUCT DESCRIPTION

BFT-1003® RM (Roof Membrane) is manufactured using DuPont® Elvaloy® BFT-1003® resin modifier. The  utilization of BFT-1003® enhances the performance of poly-vinyl chloride  (PVC) compounds by providing outstanding thermal stability and flexibility for use in more demanding applications.

USES

Especially suitable for exposed roofing

STORAGE& TRANSPORTATION

TECHNICAL INFORMATION & TESTING

| PHSICAL PROPERTITIES | TYPICAL VALUE | UNIT | TEST METHOD |
| --- | --- | --- | --- |
| Tensile Break | ≥270 | N/cm | GB12952-2011 |
| Tensile Elongation | ≥17 | % |  |
| Thermal Shrinkage | ≤0.5 | % |  |
| Bonding Strength | ≥4.0 | N/mm |  |
| Tear Strength | ≥270 | N |  |

Store and transport in the original packing, keep dry, ventilated, and out of direct sunlight.

FEATURES AND BENEFITS

- Excellent Outdoor Durability

- The outdoor service life is 20-30 years

- Excellent Mechanical Impact Resistance

- Adaptability of Thermo-cycling

- Recyclable & Environmental Friendly

STANDARD FORMAT

- Thickness: 0.9mm，1.2mm, 1.5mm

- Width：2000mm

- Length: 20m