PRODUCT DATA SHEET

Polyurethane Coating BFT-3400P

High performance polyurethane , For exterior use only

PRODUCT DESCRIPTION

BFT-3400P is a 1-part polyurethane, reinforced, cold-applied liquid membrane. It provides a flexible, seamless waterproofing solution Suitable for use in hot and tropical climatic conditions.

Uses

Designed for the following waterproofing applications:

- Roof and podium waterproofing for new construction and refurbishment projects

- Unreinforced waterproofing system for profiled metal roofs

- Reinforced waterproofing of flat and pitched roof structures, communal walkways, podium decks and roof terraces exposed to pedestrian traffic

- Waterproofing structures with numerous details, such as penetrations, drains, roof lights and complex geometry

- Waterproofing existing substrates of concrete, bituminous felt and coatings, brick, stone, asbestos cement, metal, wood, unglazed ceramic tiles

- For exterior use only

CHARACTERISTICS / ADVANTAGES

- 1-Part ready to use

- Low maintenance

- Seamless

- Easy and quick application by brush, roller or spray

- Good UV resistance and colour stability

- Retains flexibility at low temperatures

- Cold applied - requires no heat or flame

- Good elastic properties ▪

- Low temperature application > +2 °C ▪

TECHNICAL INFORMATION & TESTING

| PRODUCT INFORMATION |  |  |
| --- | --- | --- |
| Packaging | 5 GAL |  |
| Shelf Life | 12 months from date of production if stored properly. |  |
| Storage Conditions | Store dry between 40 °F (4 °C) and 95 °F (35 °C) at 50 % R.H. Place in a cool, dark and dry spot, Keep away from open flame. |  |
| PROPERTY | VALUE | TEST METHOD |
| Density | ~1.26 kg/l (value at +25 °C) | ISO/R 2811-1 |
| Solid content by volume | ~85% | ISO 3251 |
| Skintime | ≤12h | GB 19250-2013 |
| Curing time | ≤24h |  |
| CURED MECHANICAL PROPERTIES |  |  |
| Tensile Strength | 2MPa | GB/T 528 / ISO 37 |
| Elongation to Break | 450% |  |
| Tear strength | 15N/mm | GB/T 529 / ISO 34 |

Results may differ based upon statistical variations depending upon mixing methods and equipment, temperature, application methods, test methods, actual site conditions and curing conditions

Application Instructions

SURFACE PREPARATION:

Surfaces must be clean, dry and free from all traces of grease, oil and dust. As a rule, the substrates must be prepared in accordance with the instructions given in the current Primer Chart.

SUITABLE SUBSTRATES:

Cementitious, concrete, bituminous felt and coatings, brick, stone, asbestos cement,

metal, wood, unglazed ceramic tiles

MIXING

Before application, mix for at least 2 minutes or until

the liquid and all the coloured pigment have achieved a uniform colour.

CLEANING OF EQUIPMENT

Clean all tools and application equipment with Thinner C or xylene immediately after use. Hardened material can only be removed mechanically or with a proprietary paint stripper

Limitation

- Do not dilute with any solvent.

- Do not apply near to running air intakes of air conditioning units. Switch off units and seal intakes before applying.

- All areas requiring an anticorrosive protection system must be applied directly to a prepared bright metal finish

- Do not apply on substrates with rising moisture orare not stable.